## Outline: Hot-Dip, Mechanical, or Zinc Plate — Which Coating Belongs on Your Job

Category: Specifications & Standards 
SEO Title: Hot-Dip Galvanized vs. Mechanical vs. Zinc Plated Fasteners: How to Specify the Right Coating 
Meta Description: Three coatings, three different performance profiles — and they're not interchangeable. A plain-English guide to ASTM A153, B695, and B633 for fastener applications. 
Suggested Slug: /blog/hot-dip-galvanized-vs-mechanical-vs-zinc-plate-fasteners

### Opening hook

The call that comes in: a contractor has a drawing that says "galvanized" with no further specification. They order zinc-plated bolts because they're cheaper and faster. Six months later there's corrosion. This happens more than it should — because "galvanized" means three different things depending on who you ask.

### I. Why coating selection gets treated as an afterthought — and why it isn't

- Grade and diameter get all the attention on a drawing; coating is often a footnote or left unspecified

- But coating determines service life, thread fit, and whether field modifications are even possible

- The three coatings look similar out of the box. The differences show up in year two or after the first wet season.

### II. Hot-Dip Galvanizing (ASTM A153 / F2329)

- What it is: parts dipped in molten zinc at ~840°F, bonding metallurgically to the steel

- Two relevant standards: A153 covers hardware (bolts, nuts, washers), F2329 specifically covers fasteners — and they have different coating thickness requirements

- Thickness: 1.0–3.9 mils depending on material class — the thickest of the three options

- Best for: outdoor structural, anchor bolts in concrete, anything with long service life in wet or corrosive environments

- The thread fit problem: HDG adds significant material to threads — nuts must be overtapped to fit, or you need to specify HDG-compatible nut grades (A563 DH is the standard companion). This catches people off guard constantly.

- Not suitable for: high-strength fasteners over 150 ksi (hydrogen embrittlement risk during pickling)

### III. Mechanical Galvanizing (ASTM B695)

- What it is: cold process — zinc powder is tumbled onto parts with glass beads and chemical promoters, no heat involved

- Thickness: comparable to HDG at heavier classes (Class 50, 55, 65), but more controllable

- Key advantage over HDG: no hydrogen embrittlement risk — safe for high-strength fasteners (Grade 8, A490, A354 BD) that can't go through the HDG acid pickling process

- Thread fit: still adds material, but more uniform than HDG — less overtapping required

- Best for: high-strength bolts that need corrosion protection, mixed assemblies where HDG heat could cause distortion, parts with tight dimensional tolerances

- Less common in the field but important to know when it's the right answer

### IV. Zinc Electroplating (ASTM B633)

- What it is: electrochemical process depositing a thin zinc layer — typically 0.2–0.5 mils

- Thinnest of the three — provides corrosion protection in dry or mildly corrosive environments only

- Best for: interior applications, light industrial, anywhere appearance matters and the environment is controlled

- Not for outdoor structural use — the coating simply isn't thick enough for long-term exposure

- The confusion: zinc plate looks like galvanizing. The part is silver, it has a coating. But the performance gap is enormous — HDG can last 50+ years in outdoor exposure; zinc plate in the same environment might last 2–5.

- Fastest and cheapest of the three, which is why it gets substituted when it shouldn't be

### V. The field-cut problem

- When you cut hot-dip galvanized threaded rod in the field, the cut end is bare steel — the zinc coating doesn't extend past the saw line

- That bare end is now the corrosion initiation point for the whole assembly

- Shop-cut solves this: we cut before galvanizing, or we can cold-galvanize / seal the cut end in the shop

- Contractors know this and often accept it as a field reality — but on long-service applications (anchor bolts, embedded rod, coastal installations) it's worth the conversation before the job ships

### VI. Quick reference: which one do you need?

A clean decision framework — three scenarios mapped to the right coating:

| Situation | Right Call |
| --- | --- |
| Outdoor structural, long service life | Hot-dip (F2329 / A153) |
| High-strength bolts (A490, Grade 8, A354 BD) needing corrosion protection | Mechanical (B695) |
| Interior / light industrial, cost-sensitive | Zinc plate (B633) |
| Coastal, marine, or chemically aggressive environments | Stainless or duplex — no coating covers this |

### VII. When no coating is the answer

- Stainless fasteners in marine/corrosive environments outperform any carbon steel + coating combination

- Weathering steel (Cor-Ten) structures sometimes specifically exclude galvanizing — the coating interferes with the patina formation that is the corrosion protection

- Worth flagging: if the drawing calls for "galvanized" on a weathering steel job, that's a conflict worth resolving before ordering

### Closing + CTA

- The one-sentence version: hot-dip is the outdoor workhorse, mechanical fills the gap for high-strength parts, zinc plate is for interior use only — and none of them replace stainless in aggressive environments

- Link to Specification Library, Material Spec Builder, and quote form